## Modelling low field electron mobility in group III nitride materials

### Dr. H. Arabshahi

Department of Physics, Tarbiat Moallem university,  Sabzevar, Iran

Abstract

Temperature and doping dependencies of electron mobility in both wurtzite and zincblende GaN structures have been calculated using an iteravive technique. The following  scattering mechanisims, i.e, impurity, polar optical phonon, acoustic phonon, piezoelectric and electron plasmon are inculded in the calculation. Ionized imurity scattering has been treated beyound the Born approximation using the phase-shift analysis.  It is found that the electron mobility decreases monotonically as the temperature increases from 100K to 600K. The low temperature value of electron mobilty increases significantly with increasing doping concentration. The iterative results are in fair agreement with other recent calculations obtained using the relaxation-time approximation and experimental methods.

Keywords: GaN; SiC; Wurtzite; Zincblende; Plasmon

I- Introduction

Wide band gap GaN and related compounds with aluminium and indium currently have two main uses in commercial devices, providing bright LEDs emitting at ultraviolet-blue green wavelengths for CD-ROM and sensor applications and heterojunction field effect transistors (HFETs) which can sustain high current densities at elevated temperatures [1-2]. It has been shown that GaN has large peak electron velocity and can be an important candidate for high frequency application. A wide energy band gap leads to a low intrinsic carrier concentraion, which enables a more precise control of free carrier concentration over a wide range of carrier concentration over a wide range of temperatures, and hence the devices made of this kind of material will be operable at high temperatures with large breakdown voltage. The development of GaN based transport devices is hampered by the nonavailability of detailed knowledge of the transport properties and transport parameter. Keeping    in    mind   its    huge   technological  prospect, we need a better understanding of these materials. The electron drift mobility is the   most   popular   and   important   transport  parameter used to characterize the microscopic quality of epitaxial layers. There has been very little work on the  calculation of low field electron mobility in GaN, Chin et al. [3] have used the variational principle to calculate low field electron mobilities and compared their results with fairly old experimental data. They have tried to fit the experimental data with an overestimated compensation ratio.  In old samples, low electron mobility was due to poor substrate and buffer quality and other growth related problems. The iterative technique has been used by Rode and Gaskill [4] for low field electron mobity in GaAs for the dependence of mobility on electron concentration, but not on temperature, and ionized impurity scattering has been estimated within the Born approximation, which might be the reason for poor fitting at high electron concentrations.

This paper presents the iteative calculation results of electron transport in bulk GaN for both the natural wurtzite and also the zincblende lattice phases. Most of the calculations have been carried out using a non-parabolic ellipsoidal valley model to describe transport in the conduction band. However, the simpler and less computationally intensive spherical parabolic band scheme has also been applied, to test the validity of this approximation. The iterative calculations take into account the electron-lattice interaction through polar optical phonon scattering, deformation potential acoustic phonon scattering (treated as an elastic process), piezoelectric and electron plasmon scattering. Impurity scattering due to ionized and neutral donors is also included, with the latter found to be important at low temperature due to the relatively large donor binding energy which implies considerable carrier freeze-out already at liquid nitrogen tempearure.

This paper is organised as follows. Details of the iterative model and the electron mobility calculations are presented in section II, the electron scattering mechanism which have been used are discussed in section III and the results of iterative calculations carried out on GaN structures are interpreted in section IV.

# II- Model details

In principle the iterative technique give exact numerical prediction of electron mobility in bulk semiconductors. To calculate mobility, we have to solve the Boltzmann equation to get the modified probability distribution function under the action of a steady electric field. Here, we have adopted the iterative technique for solving the Boltzmann transport equation. Under application of a uniform electric field the Boltzmann equation can be written as

(eℏ)E.∇kf=[s'f'(1−f)−sf(1−f')]dk                                               (1)

where f=f(k)  and f'=f(k')  are the probability distribution functions and s=s(k,k') and s'=s(k',k) are the differential scattering rates. If the electric field is small, we can treat the change from the equilibrium distribution function as a perturbation which is first order in the electric field. The distribution in the presence of a sufficiently small field can be written quite generally as

f(k)=f0(k)+g(k)cosθ                                                                   (2)

where f0(k) is the equilibrium distribution function,  is the angle between k and E and g(k) is an isotropic function of  k, which is proportional to the  magnitude of  the electric field. In general, contributions to the differential scattering rates come from two types of scattering processes, elastic scattering sel, due to acoustic, impurity, plasmon and piezoelectric phonons, and inelastic scattering sinel, due to polar optic phonons

s(k,k')=sel(k,k')+sinel(k,k')                                                             (3)

The polar phonon energy is quite high (~92 mev) in case of GaN. Hence, this scattering process can not be treated within the framework of the relaxation time approximation (RTA) because of the possibility of the significant energy exchange between the electron and the polar optic modes. In this case, sinelrepresents transitions from the state characterized by k to k' either by emission [sem(k,k')]or by absorption [sab(k,k')] of a phonon. The total elastic scattering rate will be the sum of all the different scattering rates which are considered as elastic processes, i.e. acoustic, piezoelectric, ionized impurity, and electron-plasmon scattering. In the case of polar optic phonon scattering, we have to consider scattering-in rates by phonon emission and absorption as well as scattering-out rates by phonon absorption and emission. Using Boltzmann equation and considering all differential scattering rates, the factor g(k) in the perturbed part of the distribution function f(k) can be given by

g(k)=−eEℏ∂f0∂k+g'cosϕ[sinel'(1−f)+sinelf)]dk(1−cosϕ)seldk+[sinel(1−f')+sinel'f']dk              (4)

Note, the first term in the denominator is simply the momentum relaxation rate for elastic scattering. It is interesting to note that if the initial distribution is chosen to be the equilibrium distribution, for which g(k) is equal zero, we get the relaxation time approximation result after the first iteration. We have found that convergence can normally be achieved after only a few iterations for small electric fields. Once g(k) has been evaluated to the required accuracy, it is possible to calculate quantities such as the drift mobility which is given by

∞f(k)dk                                                          (5)

Where d is defined as 1d=m∇kEℏ2k. In the following section electron-phonon, electron-impurity and electron-plasmon scattering mechanisms will be discussed.

III- Electron scattering mechanisms

- Phonon scattering

The dominant scattering mechanism of electrons in polar semiconductors like GaN comes from the electron-phonon interaction except at the lowest temperatures. The electron-optical phonon interaction contributes both in the ohmic and non-ohmic mobility and provides the dominant energy-loss mechanism of electrons. First order polarization occurs in connection with the primitive unit cell, characteristic of the longitudinally polarized optical mode. In GaN the Debye temperature is more than 1000K [6], hence polar optical phonon scattering must be considered as an inelastic process. Other phonon scattering processes, i.e. acoustic and piezoelectric scattering are considered as elastic processes.  Like GaAs, GaN also has a single minimum valley at K= 0 ( valley). So internally phonon scattering can be neglected at low field conditions. In polar optic phonon scattering the differential scattering rates for absorption and emission can be written as [5]

Sop(k,k')=2m∗e2ωop8πε0ℏ(1ε∞−1εs)1+2αE'γ12(E)F0(E,E')Nop,(Nop+1)                                               (6)

where s  and  are define in table 1, Nop  is the phonon occupation number and the Nop and 1+Nop refer to absorption and emission, respectively. For small electric fields, the phonon population will be very close to equilibrium, so that the average number of phonons is given by the Bose-Einstein  distribution function. We have found that after a few iterations, the electron polar optical phonon scattering rate converges and becomes very close to the experimental result [6]. Also it is found that the electron polar optical phonon scattering rate in GaN is almost one order of magnitude larger than in GaAs, which can be attributed to its larger ionic properties.

The energy range involved in the case of scattering by acoustic phonons is from 0 to 2ℏvsk, as the momentum conservation restricts the phonon wave vector q between 0 and 2k , where k  is the electron wave vector. Typically the average value of k is on the order of 107 cm-1 and vs, the velocity of sound in the medium, is on the order of  105 cm/s. Hence, 2ℏvsk1 meV, which is small compared to the thermal energy. Hence electron-acoustic phonon scattering can be considered as an elastic process. Actually, a long wave length acoustic displacement can not affect the energy since neighboring unit cells move by almost the same amount, only the differential displacement (normally the strain) is of importance. The total differential scattering rate for acoustic phonons can be given by

Sac(k,k')=2Dac2(mtml)12KBTπρv2ℏ4E(1+αE)(1+2αE)[(1+αE)2+13(αE)2]                               (7)

where Dac is the acoustic deformation potential,  is the material density and  is the non-parabolicity coefficient.  The formula clearly shows that the acoustic scattering increases with temperature.

In crystals like GaN, whose lattice lacks inversion symetry, such as those semiconductors with sphacelate or wurtzite structure, elastic strain may be accompanied by macroscopic electric fields. This piezoelectric effect provides an additional coupling between the electric and acoustic vibrations. The differential scattering rate for piezoelectric scattering will be

Spz(k,k')=m∗e2Kac2KBT42πε0εsℏ2γ−12(E)(1+2αE)2×Ln(1+8mγ(E)ℏ2q02)                                 (8)

where Kav is the dimensionless so called average electromechanical coupling constant [7].

- Impurity scattering

The standard technique for dealing with ionized impurity scattering in semiconductors is the Brook-Herring (BH) technique [8], which is based on two inherent approximations. First, is the first order Born approximation and second is the single ion screening approximation. These two approximations essentially lead to a poor fit to the experimental mobility data [9,10]. Several attempts have been made to modify the BH technique phenomenologically [11]. It has been shown that phase-shift analysis of electron-impurity scattering is the best way to overcome the Born approximation. Departure from the BH prediction of electron mobility is evident at higher electron concentrations. Meyer and Bartoli [9] have provided an analytic treatment based on phase-shift analysis taking into account the multi-ion screening effect and finally been able to overcome both the approximations. All the previous techniques of impurity screening by free electrons in semiconductors were based on the Thomas-Fermi (TF) approximation which assures that a given impurity should be fully screened. The breakdown of the single-ion screening formalism becomes prominent in the strong screening regime, where the screening length calculated through TF theory becomes much shorter than the average distance between the impurities and hence neighboring potentials do not overlap significantly. This essentially leads to a physically unreasonable result. In the case of high compensation, the single-ion screening formalism becomes less relevant, because in order to maintain the charge neutrality condition, it would be more difficult for a given number of electrons to screen all the ionized donors separately. In the case of GaN, the compensation ratio is usually quite large, and the ratio ND+n is also temperature dependent. Hence the multi-ion screening correction is very essential in GaN. The effective potential of an ionized impurity scattering center is spherically symmetric in nature, so one can use phase-shift analysis to find the differential scattering rate s(k,k') more accurately. The effective potential V(r)due to an ionized impurity can be expressed as V(r)=−(Zle2)(4πε0κ0r)e−rλ, where Zl is the charge of the ionized impurity in units of e and  is the screening length. The standard technique to find out the screening length is the TF approach which is based on single ion screening approximation. In TF one can calculate the charge contribution qi to the screening of a single ionized donor by an electron of energy Ei and is given by qi=−(2e3λ2ε0κ0EiV). In the case of multi-ion problem, the TF approach can be generalized to find out the effective charge contribution due to an electron to screen all ionized donors and can be given by Qi=−(2e3ND+λ2ε0κ0Ei). Total screening charge exactly neutralizes the ionized donors, when Qi is summed over all electronic states

IEE REVIEW     (Conf. Proc., Vol. 129, I, No. 1, DECEMBER 2003)

i−Qief0(Ei)=ND+                                                                           (9)

For the sufficiently low energy electrons, Qi can be greater than the electronic charge, which is physically unreasonable. One way to tackle [9] this problem is to introduce a  factor Si such that

Si(Ei)=Eiξ         Ei⟨ξ                                                                                (10)

where ξ=(2ND+c2λ2ε0k0), Qi  will be modified to Qi'=QiSi in Eq. (9). For the low energy electrons the contribution will be –e. Since the total contribution to the screening by the low energy electrons has been effectively decreased, Eq. (9) no longer holds. However, if the screening length  is more than the average distance between the donors, it is not necessary to insist that each donor be fully screened, only it is required that overall charge neutrality should be preserved. Electrons in the overlap region can provide screening to both the ionized donors. Here we can define a factor p, which would be the fraction of the total charge, which is contained within a sphere of radius R surrounding the donor. Hence Eq. (9) will be modified as

i−Qi} } }  over  {e} } f rSub { size 8{0} }  \( E rSub { size 8{i} }  \) = ital pN rSub { size 8{D} }  rSup { size 8{+{}} } } } {                                                                                            (11)

where Qi} } = ital pQ rSub { size 8{i} } S rSub { size 8{i} } } {. The screening charge requirement will be fulfilled by adjusting the screening length untill Eq. (11) is satisfied and is given by

λm−2=ηλ0−2                                                                                                   (12)

where m is multi-ion screening length and 0 is TF screening length. The differential scattering rate for ionized impurity can be given as

Sii(k,k')=8π3ℏ3m2V2f(X)2δ[E(k')−E(k)]                                                        (13)

where scattering amplitude f(X) depends on the phase shift l and Legendre polynomial Pl and is given by

f(X)=12ikl=0∞(2l+1)(e2iδl−1)Pl(X)                                                (14)

It has already been mentioned that in n-type GaN the activation energy of the donors is quite large, which keeps a large number of donors neutral at low temperatures. Neutral impurity scattering has been dealt with previously using the Erginsoy [12] expression which is based on electron scattering by a hydrogen atom and a scaling of the material parameters. It has been shown that an error as high as 45% results in the neutral impurity scattering cross section with this simple model. Meyer and Bartoli [9] have given a phase shift analysis treatment based on the variational results of Schwartz [13] to calculate the neutral impurity cross section, which is applicable for a larger range of electron energy.

- Plasmon scattering

Though carrier mobility and various scattering phenomena in semiconductor have been studied extensively, there is hardly any study regarding the effect of electron-plasmon scattering on electron mobility except the excellent work by Fischetti in the case of  Si [14]. He has shown that the electron-plasmon interaction is important at doping densities above 1017 cm-3. Plasmons are the collective excitations of the free electrons against the positive background charges, and creat long range electric fields (like LO polar optic phonons) which can scatter the electrons. In the case of electron-plasmon scattering, electrons can gain momentum from colective excitations, but it may be returned to electrons if plasmons decay into single particle excitations, which is called Landau damping. Electron mobility is affected indirectly by modifying the distribution function if Landau damping is the faster decay channel. When plasmons decay through collisions with phonons and impurities, it can directly affect the electron mobility. It has been shown [14] that if decay due to collisional damping dominates over Landau damping, electron-plasmon scattering can reduce the electron mobility by 20% for electron concentrations greater than 1017 cm-3. The differential scattering rate for an electron of wave vector k and energy E to absorb or emit a plasmon of energy ℏω is given by

Se−p(k,k')=Θ(E')ωk'(1+2αE')a01−f0(E')1−f0(E)Np(ω)+12∓12×1−k'φ(E')kφ(E)X1q2dX                               (15)

where upper and lower signs represent absorption and emision, respectively. Xc=[1+Ψ−(qck)22Ψ12], qc is the maximum value of the plasmon wave vector, above which plasma oscillation can not be sustained. The usual

approximation is qc=1λ0. Θ(E')is the step function, where E'=E±ℏω, NP(ω)=1[exp(ℏωkBT)−1] is the Bose occupation number of the plasmons. q is the plasmon wave vector given by q2=k2(1+Ψ−2Ψ12X) and Ψ=(k'/k)2=(1±ℏωE)(1+αE')(1+αE). φ(E)=τ(E)(1+2αE), where τ(E) is the total relaxation time. To evaluate the integral in Eq.15 requires the solution of the nonlinear Boltzmann equation. It has been shown [8]  that the energy dependence of φ can be ignored for the entire electron concentration range of interest, which means that φ(E')φ(E)≈1. The total plasmon momentum relaxation rate is given by

νe−p=g(ωp−ω)1τpl(E,ℏω)d(ℏω)                                           (16)

where ωp=ωp0(1−3αℏωp0)is the plasma frequency corrected for the nonparabolicity effect and ωp02=ne2εm is the plasma frequency. g(ωp−ω)=Γπ[(ℏωp−ℏω)2+Γ2], where  is the half width of the plasmon line due to Landau damping and is small at large impurity concentrations because the decay rate is inversely proportional to the plasma energy. The half width due to collision damping can be estimated by the single particle relaxation rate. We do not need to determine relaxation rate exactly, because mobility depends very weakly on  as long as the damping is not too strong.

IV- Results and discussion

We have performed a series of low-field electron mobility calculations for both the natural wurtzite and the zincblende lattice phases of GaN. Low-field mobilities have been derived using iteration methode. Important parameters used throughout the calculations  are listed in table 1, which are taken from Ref. [15,16].

| Parameter | zincblende | wurtzite |
| --- | --- | --- |
| Band-gap (eV) Electron effective mass (m* ) m║ (-A) m ( - M) Nonparabolicity (eV-1 ) Static relative permitivity 0 Optical relative permitivity  Density (kgm-3 ) Sound velocity (ms-1 ) Deformation potential (eV) Piezoelectric constant (Cm-2 ) Optical phonon energy (eV) | 3.2 0.15 0.15 0.213 9.5 5.35 6100 4570 8.3 0.375 0.0995 | 3.5 0.18 0.2 0.189 9.5 5.35 6150 4330 8.3 0.375 0.0995 |

Table 1. Important parameters used in our calculations

for  zincblende and wurtite GaN

Figure 1 shows reasonably good agreement between experimental and calculated mobility-temperature dependencies in both structures. For wurtzite structure the calculations have been performed for an electric field applied along the -A (c-axis, c-GaN)  and -M (parallel to basal plane, h-GaN) directions of the Brillouin zone. The peak electron drift mobility in two directions are, respectively, 1300 cm2/V-s and 1100 cm2/V-s at room temperature. The reason for this difference can be explained as follows. The  valley effective mass is greater in the  -M direction than -A, which implies that an electric field applied perpendicular to the c-axis will be less efficient in heating the electron ensemble. It can be seen from the figure that the electron drift mobilities at room temperature that we find are 1300 and 1800 cm2/V-s for wurtzite and zineblende structures, respectively, for an electric field equal to 104 Vm-1 and with a donor concentration of 1022 cm-3. The results plotted in figure 1 indicate that the electron drift mobility of wurtzite GaN is lower than zincblende structure at all temperatures. This is largely due to the higher  valley effective mass in the wurtzite phase.

Fig.1. Electron drift mobility of GaN in zinceblende and wurtzite structures (both perpendicular to c-axis and parallel to c-axis) versus temperature. Donor concentration is approximately 1022 cm-3.

IEE REVIEW     (Conf. Proc., Vol. 129, I, No. 1, DECEMBER 2003)

Figure 2 shows the calculated variation of the electron mobility as a function of the donor concentration for both GaN crystal structures at room temperature. The mobility does not vary monotonically between donor concentrations of 1021 cm-3 and 1025 cm-3  due to the dependence of electron scattering on donor concentration, but shows a maximum near 1021 cm-3 for zincblende and wurtzite.

Fig.2. Calculated low-field electron drift mobility of zincblende and wurtzite GaN (c-GaN) as a functions of different donor concentrations at room temperature.

In figure 3, the electrons as a function of temperature using the screened shallow donor binding energy results of Wang, et al. [17] for different background electron concentrations. The temperature effects on the carrier screening are taken into account for this calculation. The figure clearly shows that for uncompensated GaN at liquid nitrogen temperature there is a large fraction of neutral donor impurities present.

Fig.3. Electron concentration versus temperature for c-GaN with different donor doping densities.

IEE REVIEW     (Conf. Proc., Vol. 129, I, No. 1, DECEMBER 2003)

The temperature variation of the electron drift mobility in zinceblende and wurtzite GaN (c-GaN) for different donor concentrations is shown in figure 4. It is evident from this figure that the curves approach each other at very high temperatures, where the mobility is limited by longitudinal optical phonon scattering, whereas the mobility varies inversely with donor concentration at low temperature, as we would expect from the foregoing discussion. The decrease in mobility at low temperature is caused in part by neutral impurity scattering. For the lowest doping concentration considered in this calculation,  1021 cm-3, we find that the neutral impurity scattering plays a large role at low temperature because of the significant carrier freeze-out evident from figure 3.

Fig.4. Electron drift mobility versus temperature for zincblende and c-GaN with different donor doping densities.

V- Summary

In conclusion, we have quantitatively obtained temperature-dependent and electron concentration-dependent electron mobility in both zincblende and wurtzite GaN structures using an iteravive technique. The theoretical values show good agreement with recently obtained experimental data. It has been found that the low-field mobility is significantly higher for the wurtzite structure than zincblende due to the higher electron effective mass in the wurtzite crystal structure. Several scattering mechanisms have been included in the calculation including electron-plasmon scattering. Ionized impurities have been treated beyond the Born approximation using a phase shift analysis. Screening of ionized impurities has been treated more realistically using a multi-ion screening formalism, which is more relevant in the case of highly compensated III-V semiconductors like GaN and SiC.

Acknowledgments

This work benefited from useful discussion with G. Crow. A grant from the Tarbiat Moallem University of Sabzevar is gratefully acknowledged.

#### Refferences

[1]  S Nakamura, M Senoh and T Mukai,  Appl.  Phys. Lett. 62,  2390

(1993)

[2]  S Strite and H Morkoc,  J. Vac. Sci. Technol.  B 10,  1237 (1992)

[3]  V W L Chin and T L  Tansley, J. Appl. Phys.  75,  7365 (1994)

[4]  D L Rode and D K Gaskill, Appl. Phys. Lett.   66,  1972 (1995)

[5] C Moglestue, Monte Carlo simulation of  semiconductor devices,

Chapman and Hall   (1993)

[6]  K T Tsen, D K Ferry, A Botchkarev, B Suerd,  A Salvador

and H Morkoc, Appl.  Phys. Lett.  71,  1852 (1997)

[7] B K Ridley, Electrons and phonons in  semiconductor

multilayers, Cambridge  University press (1997)

[8]  H Brooks, Phys. Rev.  83,  879 (1951)

[9]  J R Meyer and F J Bartoli, Phys. Rev. B 23,  5413 (1981)

[10]  J R Meyer and F J Bartoli ,   Solid State  State Commun. 41, 19

(1982)

[11]  D Chattopadhya and H J Queisser, Rev.  Mod. Phys. 53, 745

(1981)

[12]  C Erginsoy, Phys. Rev. 79,  1013 (1950)

[13]  C Schwartz, Phys. Rev. 124,  1468 (1961)

[14]  M V Fischetti, Phys. Rev.  44,  5527 (1991)

[15]  H Morkoc, Nitride semiconductor and devices, Springer-velag

(1999)

[16]  Udayan, V Bhapkar and M S Shur, J. Appl.  Phys.  82,  1649

(1997)

[17]  R P Wang, P P Ruden, J Kolnik and K F Brennan, Mat.

Res. Soc. Symp. Proc.,  445,  935 (1997)